Estonian Plywood AS Quality Requirements to Birch Logs

| Quality class | BC | BC |  |  | A |  |
| --- | --- | --- | --- | --- | --- | --- |
| Log diameter under bark (cm) | 12-15 | 16-17 | 18+ | 24+ |  |
| Log length +oversize | 2.7m; 3.2m; 4.8m Minimum oversize 6cm, maximum oversize 30cm |  |  |  |  |  |
|  | Minimum oversize allowed if the log end surfaces are free of defects and need not be crosscut again. Maximum diameter of the thickest trunk section measured from the bark 0.6m. |  |  |  |  |  |
| Sound knots | Allowed | Allowed |  |  | Not allowed |  |
| Dry knots | d ≤ 20mm | d ≤ 40mm |  |  | Not allowed |  |
| Rotten knots | d ≤ 20mm | d ≤ 40mm |  |  | Not allowed |  |
| Intergrown knots | Allowed | Allowed |  |  | Allowed |  |
| Epicormic knot | Not allowed | Sound branch d ≤ 50mm and up to 150mm long; dry or rotten d ≤ 20mm wide and 60mm long | Sound branch d ≤ 80mm and up to 240mm long; dry or rotten d ≤ 40mm and 120mm long | Not allowed |  |
|  | A knot under 10mm is not considered a defect; the knot diameter is measured from the log surface perpendicularly to the longitudinal axis of the log |  |  |  |  |  |
| Single curvature | The straightness of the entire log is assessed. Curvature is only allowed for module (1.3 or 1.6m) at the cut 20mm | 40mm (assessed on module) | allowed single curvature of log d < 240mm is 50mm (assessed on module); log d≥ 240mm allowed single curvature 60mm | 50mm (assessed on module) |  |
| Compound curvature | Not allowed | Not allowed | Not allowed | Not allowed |  |
|  | A log is too warped if the line connecting log end centres runs outside the log and the module centreline runs beyond another module |  |  |  |  |  |
| End shake, ring shake | End shakes: a) heart shake – from bark to bark excl. under 2mm; b) ring shake is allowed as semicircle (180 degrees). Side shakes must not extend into the processing cylinder | End shakes: a) heart shake – from bark to bark excl. under 2mm; b) ring shake is allowed as semicircle (180 degrees). Side shakes must not extend into the processing cylinder |  |  | End shakes: a) heart shake – from bark to bark excl. under 2mm; b) ring shake is allowed as semicircle (180 degrees). Side shakes must not extend into the processing cylinder |  |
| Frost crack, lightning crack | Not allowed | Not allowed |  |  | Not allowed |  |
|  | Cracks must not extend to the nominal length, cracks are allowed to the length of the oversize |  |  |  |  |  |
| Red heart, hard rot | Allowed | Allowed |  |  | Allowed up to 1/3 of the diameter (must be located in the centre of the log end surface) |  |
| Burl | May not extend into trunk timber | May not extend into trunk timber |  |  | May not extend into trunk timber |  |
| Intact bark pocket without rot | Not allowed | Allowed on one side of a log with a length up to 60cm, depth up to 10% of the processing cylinder |  |  | Not allowed |  |
| Soot | Not allowed | Allowed on bark (fire damage must not extend into the processing cylinder); charred wood is not allowed |  |  | Not allowed |  |
| Foreign bodies, deadwood, soft rot, storage rot, discoloration, | Not allowed | Not allowed |  |  | Not allowed |  |
| Branch stumps | Height up to 30mm | Height up to 50mm |  |  | Not allowed |  |
| Butt swell, fluting | Not allowed | Allowed depth up to 50mm |  |  | Allowed depth up to 30mm |  |
| Mechanical damage and rupture (incl. felling and/or crosscutting cracks) | Not allowed | Length up to 60 cm, depth up to 10% of the processing cylinder |  |  | Not allowed |  |